## Slide 1
Annealing effects on the mechanical losses of fluorides thin films
Amato Alex1
Bischi Matteo2,3
Forest Danièle1
Granata Massimo1
Guidi Gianluca Maria2,3
Martelli Filippo2,3
Mereni Lorenzo1
Piergiovanni Francesco2,3
1LMA, CNRS
2Università di Urbino
3INFN
Matteo Bischi GRASS, Padova 17.10.2019

## Slide 2
Matteo Bischi GRASS, Padova 17.10.2019
Outlook
Why using Fluorides?
Experimental work
What is left to do
Conclusions

## Slide 3
Matteo Bischi GRASS, Padova 17.10.2019
Why using Fluorides?
Coating thickness
Temperature
Loss angle
Young’s Modulus
Frequency
Laser beam width
Ti(20%):Ta2O5 n = 2.07 φ = 3 x 10-4
SiO2 n = 1.45 φ = 4 x 10-5

## Slide 4
Matteo Bischi GRASS, Padova 17.10.2019
Why using Fluorides?
Room Temperature
Fluorides like MgF2 have the lowest refractive index (n = 1.4) among the known coating materials

## Slide 5
Matteo Bischi GRASS, Padova 17.10.2019
Experimental Work - GeNS

## Slide 6
Experimental Work - GeNS
Linear fit
Exponential decay of the amplitude
Matteo Bischi GRASS, Padova 17.10.2019

## Slide 7
Experimental Work - Annealing
Matteo Bischi GRASS, Padova 17.10.2019
A succession of annealing treatments were performed on silica disks coated with MgF2 on both sides. The annealing was done inside a tube furnace in a controlled Argon atmosphere, in order to prevent the oxidation of the coating.
After each annealing cycle, the loss angle and the weight of the sample were measured, in order to extract the coating losses.

## Slide 8
Matteo Bischi GRASS, Padova 17.10.2019
Experimental Work - Samples
Substrate thickness | 1 mm
Substrate diameter | 50 mm
Substrate mass | (4.6158 ± 0.0001)g
Coating thickness (on each side) | 206 nm
Total mass (substrate + coating) | (4.6179 ± 0.0001)g
MgF2 thin layers were deposited on both sides of silica substrates by ion beam sputtering at the Laser Zentrum Hannover. The measured thickness of each layer is 206 nm. The samples were also edge-polished using a CO2 laser.

## Slide 9
Matteo Bischi GRASS, Padova 17.10.2019
Experimental Work
Two kinds of experiments performed on two different samples:
Same annealing time but different annealing temperatures
Same annealing temperature but different annealing times

## Slide 10
Matteo Bischi GRASS, Padova 17.10.2019
Annealing treatments on the first sample of MgF2 (C21025)
 | Run #1 | Run #2 | Run #3 | Run #4 | Run #5
Annealing Temperature (Tmax) | 200°C | 300°C | 400°C | 430°C | 500°C
Duration (Tmax) | 10h | 10h | 10h | 10h | 10h
Experimental Work – C21025

## Slide 11
Matteo Bischi GRASS, Padova 17.10.2019
Experimental Work – C21025

## Slide 12
 | Run #1 | Run #2 | Run #3 | Run #4
Annealing Temperature (Tmax) | 400°C | 400°C | 400°C | 400°C
Duration (Tmax) | 10h | 20h | 30h | 64h
Cumulative duration (Tmax) | 10h | 30h | 60h | 124h
Matteo Bischi GRASS, Padova 17.10.2019
Annealing treatments on the second sample of MgF2 (C21011)
Experimental Work – C21011

## Slide 13
Matteo Bischi GRASS, Padova 17.10.2019
Experimental Work – C21011

## Slide 14
Matteo Bischi GRASS, Padova 17.10.2019
Experimental Work
We can find the loss angle of the coating (c) measuring the bare substrate (s) and the coated substrate (s+c):
Where «D» is called Dilution Factor and is evaluated by:

## Slide 15
Matteo Bischi GRASS, Padova 17.10.2019
Experimental Work
Resonance frequency variation due to temperature variation
From the slope we obtained:
k = 1.58 x 10-4
And we can correct the values of the resonance frequencies by an amount:

## Slide 16
Matteo Bischi GRASS, Padova 17.10.2019
What is left to do
Understand why the loss angle of the coating increases at annealing temperatures above 430°C
Hypothesys:
Crystallization of MgF2 took place (a new XRD analysis will be repeated soon)
Cracks on the surface of the MgF2 films due to differences of thermal expansion coefficients between the substrate and the coating

## Slide 17
Matteo Bischi GRASS, Padova 17.10.2019
What is left to do
Upgrade of the GeNS system to operate at cryogenic temperatures and measure another set of samples coated with MgF2.
Inner tank
Copper shield
Outer tank
Liquid nitrogen/helium

## Slide 18
First Sample (C21025): after each annealing cycle the loss angle of the MgF2 coating decreases until the treatment at 430°C. Above this temperature φ increases.
Second Sample (C21011): after each annealing cycle the loss angle of the coating decreases until 60 hours of cumulative time.
Mechanical loss values of MgF2 coating are more than an order of magnitude higher than silica at room temperature, but we need to repeat measurements at cryogenic temperatures.
Matteo Bischi GRASS, Padova 17.10.2019
Conclusions

## Slide 19
Matteo Bischi GRASS, Padova 17.10.2019
Thank you!