## Slide 1: Molecular Dynamics simulations of microscopic dissipation in Ta2O5
F. Puosi, F. Fidecaro, S. Capaccioli, D. Pisignano and D. Leporini
Physics Department “E. Fermi”, University of Pisa
INFN-Pisa

## Slide 2: Ta2O5 model and simulation details
Ta
O
Classical MD simulations
Interatomic potential:
  - BKS potential (Coulomb + exponential repulsion + VdW attraction)
  - covalent bonding (Morse potential)
  [Trinastic et al., JCP 2013]
  - optimization: Wolf truncation with cut-off
  [Damart et al. JAP 2016]

## Slide 3: Mechanical loss in Ta2O5 glass
testo
Molecular Dynamics – Mechanical Spectroscopy (MD-MS)
- apply numerical strain and compute stress
F. Puosi et al., Phys. Rev. Res., in press

## Slide 4: Microscopic perspective on dissipation
We focus on and
Color code: magnitude of instantaneous velocity

## Slide 5: Statistics of plastic atomic rearrangements
Dissipation as due to irreversible events leading to change of basin in the PEL
atom displacement (in IS) over one strain cycle
Representative map of the field
Power-law distribution for
Oxygen atoms are more mobile than tantalum ones

## Slide 6: Statistics of plastic atomic rearrangements
Focus on polyhedra centered on the 5% Ta atoms with largest plastic displacement

## Slide 7: Statistics of plastic atomic rearrangements
- Plastic events involves dozens of atoms
  importance of medium range order.
slope = -2.3
cluster analysis
Corner sharing connections dominates in plastically rearranging cluster
Corner
Edge
Face

## Slide 8: Summary
Thanks for your attention
Modeling and simulations can be of valuable help in the selection and design of advanced materials for coatings application as they can:
- provide a quick estimate of losses (Q) *
- give a microscopic insight in the dissipation mechanisms,
* F. Puosi et al., Phys. Rev. Res., in press